Electron & Hole Statistics in Semiconductors More Details
Electron & Hole Statistics in Semiconductors More Details

---
NOTE!!
Much of what follows (including the color scheme) was borrowed from a lecture posted on the web by Prof. Beşire GÖNÜL in Turkey.
Her lectures are posted Here: http://www1.gantep.edu.tr/~bgonul/dersnotlari/.
Her homepage is Here: http://www1.gantep.edu.tr/~bgonul/.

---
CHAPTER 3 CARRIER CONCENTRATIONS IN SEMICONDUCTORS
CHAPTER 3
CARRIER CONCENTRATIONS IN SEMICONDUCTORS
Prof. Dr. Beşire GÖNÜL

---
CARRIER CONCENTRATIONS IN SEMICONDUCTORS
CARRIER CONCENTRATIONS IN SEMICONDUCTORS
- Donors and Acceptors
- Fermi level , Ef
- Carrier concentration equations
- Donors and acceptors both present

---
Donors and Acceptors
Donors and Acceptors
The number of carriers are generated by thermally or electromagnetic radiation for a pure s/c.
- The conductivity of a pure (intrinsic) s/c is low due to the low number of free carriers.
For an intrinsic semiconductor
n = p = ni
n = concentration of electrons per unit volume
p = concentration of holes per unit volume
ni = the intrinsic carrier concentration of the semiconductor under consideration.

---
n.p = ni2
n.p = ni2
n = p
number of e-’s in CB = number of holes in VB
This is due to the fact that when an e- makes a transition to the CB, it leaves a hole behind in VB. We have a bipolar (two carrier) conduction and the number of holes and e- ‘s are equal.
n.p = ni2
This equation is called as mass-action law.

---
n.p = ni2
The intrinsic carrier concentration ni depends on;
- the semiconductor material, and
- the temperature.
For silicon at 300 K, ni has a value of 1.4 x 1010 cm-3.
Clearly , equation (n = p = ni) can be written as
n.p = ni2
This equation is valid for extrinsic as well as intrinsic material.

---
What is doping and dopants impurities ?
What is doping and dopants impurities ?
To increase the conductivity, one can dope pure s/c with atoms from column lll or V of periodic table. This process is called as doping and the added atoms are called as dopants impurities.
There are two types of doped or extrinsic s/c’s;
n-type
p-type
Addition of different atoms modify the conductivity of the intrinsic semiconductor.

---
p-type doped semiconductor
Si + Column lll impurity atoms
Electron
Boron (B)
has three valance e-’ s
Have four valance e-’s
Hole
Si
Bond with missing
electron
Si
B
Si
Boron bonding in Silicon
Boron sits on a lattice side
Normal bond with two electrons
Si
p >> n

---
- Boron(column III) atoms have three valance electrons, there is a deficiency of electron or missing electron to complete the outer shell.
- This means that each added or doped boron atom introduces a single hole in the crystal.
There are two ways of producing hole
1) Promote e-’s from VB to CB,
2) Add column lll impurities to the s/c.

---
Energy Diagram for a p-type s/c
Energy Diagram for a p-type s/c
CB
Ec = CB edge energy level
acceptor
(Column lll) atoms
Eg
EA= Acceptor energ level
Ev = VB edge energy level
VB
Electron
Hole
The energy gap is forbidden only for pure material, i.e. Intrinsic material.

---
p-type semiconductor
The impurity atoms from column lll occupy at an energy level within Eg . These levels can be
1. Shallow levels which is close to the band edge,
2. Deep levels which lies almost at the mid of the band gap.
If the EA level is shallow i.e. close to the VB edge, each added boron atom accepts an e- from VB and have a full configuration of e-’s at the outer shell.
These atoms are called as acceptor atoms since they accept an e- from VB to complete its bonding. So each acceptor atom gives rise a hole in VB.
The current is mostly due to holes since the number of holes are made greater than e-’s.

---
Holes         =   p   =   majority carriers Electrons   =   n   =   minority carriers
Majority and minority carriers in a p-type semiconductor
Holes	= p = majority carriers
Electrons	= n = minority carriers
Electric field direction
t1
Holes movement as a
function of applied electric field
t2
t3
Hole movement direction
Electron movement direction

---
Ec
Electron
Eg
Ea
Si
Weakly bound electron
Ev
Electron
Si
P
Si
Hole
Shallow acceptor in silicon
Si
Normal bond with two electrons
Phosporus bonding in silicon

---
Conduction band
Ec
Ec
Ea
Ed
Neutral donor centre
İonized (+ve)
donor centre
Eg
Band gap is 1.1 eV for silicon
Ev
Ev
Valance band
Ec
Neutral acceptor centre
İonized (-ve)
acceptor centre
Electron
Shallow donor in silicon
Ea
Ev
Electron
Hole
Donor and acceptor charge states

---
n-type semiconductor
Si
Si
As
Extra e- of column V atom is weakly attached to its host atom
Si
Si
Si + column V (with five valance e- )
Ec
ED = Donor energy level (shallow)
Eg
ionized (+ve)
donor centre
Band gap is 1.1 eV for silicon
Electron
Ev
Hole
n - type semiconductor

---
np , pn
np , pn
n-type , n >> p ; n is the majority carrier	concentration nn
p is the minority carrier	concentration pn
p-type , p >> n ; p is the majority carrier	concentration pp
n is the minority carrier	concentration np
np pn
Type of semiconductor

---
calculation
calculation
Calculate the hole and electron densities in a piece of p-type silicon that has been doped with 5 x 1016 acceptor atoms per cm3 .
ni = 1.4 x 1010 cm-3 ( at room temperature)
Undoped
n = p = ni
p-type ; p >> n
n.p = ni2 NA = 5 x 1016 p = NA = 5 x 1016 cm-3
size 12{n= { {n rSub { size 8{i} } rSup { size 8{2} } } over {p} } = { { \( 1 "." 4x"10" rSup { size 8{"10"} } ital "cm" rSup { size 8{ - 3} } \) rSup { size 8{2} } } over {5x"10" rSup { size 8{"16"} } ital "cm" rSup { size 8{ - 3} } } } =3 "." 9x"10" rSup { size 8{3} } } {}
electrons per cm3
p >> ni and n << ni in a p-type material. The more holes you put in the less e-’s you have and vice versa.

---
Fermi level , EF
Fermi level , EF
- This is a reference energy level at which the probability of occupation by an electron is ½.
- Since Ef is a reference level therefore it can appear anywhere in the energy level diagram of a S/C .
- Fermi energy level is not fixed.
- Occupation probability of an electron and hole can be determined by Fermi-Dirac distribution function, FFD ;
EF	= Fermi energy level
kB	= Boltzman constant
T	= Temperature
size 12{F rSub { size 8{ ital "FD"} } = { {1} over {1+"exp" \( { {E - E rSub { size 8{F} } } over {k rSub { size 8{B} } T} } \) } } } {}

---
Fermi level , EF
size 12{F rSub { size 8{ ital "FD"} } = { {1} over {1+"exp" \( { {E - E rSub { size 8{F} } } over {k rSub { size 8{B} } T} } \) } } } {}
- E is the energy level under investigation.
- FFD determines the probability of the energy level E being occupied by electron.
- determines the probability of not finding an electron at an energy level E; the probability of finding a hole .
alignl { stack { size 12{ ital "if" matrix { E=E rSub { size 8{F} } widevec {} } f rSub { size 8{ ital "FD"} } = { {1} over {1+"exp"0} } = { {1} over {2} } } {} # {} # 1 - f rSub { size 8{ ital "FD"} } {} } } {}

---
Carrier concentration equations
Carrier concentration equations
The number density, i.e., the number of electrons available for conduction in CB is
The number density, i.e., the number of holes available for conduction in VB is

---
Donors and acceptors both present
Donors and acceptors both present
- Both donors and acceptors present in a s/c in general. However one will outnumber the other one.
- In an n-type material the number of donor concentration is significantly greater than that of the acceptor concentration.
- Similarly, in a p-type material the number of acceptor concentration is significantly greater than that of the donor concentration.
- A p-type material can be converted to an n-type material or vice versa by means of adding proper type of dopant atoms. This is in fact how p-n junction diodes are actually fabricated.

---
Worked example
Worked example
How does the position of the Fermi Level change with
1. increasing donor concentration, and
2. increasing acceptor concentration ?
We shall use equation
İf n is increasing then the quantity EC-EF must be decreasing i.e. as the donor concentration goes up the Fermi level moves towards the conduction band edge Ec.

---
Worked example
But the carrier density equations such as;
aren’t valid for all doping concentrations! As the fermi-level comes
to within about 3kT of either band edge the equations are no longer
valid, because they were derived by assuming the simpler Maxwell
Boltzmann statics rather than the proper Fermi-Dirac statistic.
alignl { stack { size 12{n=2 left ( { {2πm rSub { size 8{n} } rSup { size 8{*} } ital "kT"} over {h rSup { size 8{2} } } } right ) rSup { size 8{ { {3} over {2} } } } "exp" - left ( { {E rSub { size 8{c} } - E rSub { size 8{F} } } over { ital "kT"} } right )`~ ital "and"} {} # {} # p=n rSub { size 8{i} } "exp" left ( { {E rSub { size 8{i} } - E rSub { size 8{F} } } over { ital "kT"} } right ) {} } } {}

---
Worked example
Worked example
n1
n2
n3
EC
EF2
EF3
EF1
Eg/2
Eg/2
Eg/2
EV
n3 > n2 > n1
EC
Eg/2
Eg/2
Eg/2
EF1
EF3
EF2
EV
p1
p2
p3
p3 > p2 > p1

---
Worked example
(b) Considering the density of holes in valence band;
It is seen that as the acceptor concentration increases, Fermi-level
moves towards the valance band edge. These results will be used in
the construction of device (energy) band diagrams.
size 12{p=N rSub { size 8{v} } "exp" - left ( { {E rSub { size 8{F} } - E rSub { size 8{V} } } over { ital "kT"} } right )} {}

---
Donors and acceptor both present
Donors and acceptor both present
In general, both donors and acceptors are present in a piece of a semiconductor although one will outnumber the other one.
The impurities are incorporated unintentionally during the growth of the semiconductor crystal causing both types of impurities being present in a piece of a semiconductor.
How do we handle such a piece of s/c?
1) Assume that the shallow donor concentration is significantly greater	than that of the shallow acceptor concentration. In this case the material behaves as an n-type material and
2) Similarly, when the number of shallow acceptor concentration is signicantly greater than the shallow donor concentration in a piece of a s/c, it can be considered as a p-type s/c and

---
Donors and acceptor both present
Donors and acceptor both present
For the case NA>ND , i.e. for p-type material

---
Donors and acceptor both present
majority
minority

---
Donors and acceptor both present
For the case ND>NA , i.e. n-type material

---
size 12{k rSub { size 8{B} } =1 "." "38" times "10" rSup { size 8{ - "23"} } " JK" rSup { size 8{"-1"} } } {}
a) Energy level diagrams showing the excitation of an electron from the valence band to the conduction band.
The resultant free electron can freely move under the application of electric field.
b) Equal electron & hole concentrations in an intrinsic semiconductor created by the thermal excitation of
electrons across the band gap
Optical Fiber communications, 3rd ed.,G.Keiser,McGrawHill, 2000

---
n-Type Semiconductor
n-Type Semiconductor
Donor level in an n-type semiconductor.
The ionization of donor impurities creates an increased electron concentration distribution.
Optical Fiber communications, 3rd ed.,G.Keiser,McGrawHill, 2000

---
p-Type Semiconductor
p-Type Semiconductor
Acceptor level in an p-type semiconductor.
The ionization of acceptor impurities creates an increased hole concentration distribution
Optical Fiber communications, 3rd ed.,G.Keiser,McGrawHill, 2000

---
Intrinsic & Extrinsic Materials
Intrinsic & Extrinsic Materials
- Intrinsic material: A perfect material with no impurities.
- Extrinsic material: donor or acceptor type semiconductors.
- Majority carriers: electrons in n-type or holes in p-type.
- Minority carriers: holes in n-type or electrons in p-type.
- The operation of semiconductor devices is essentially based on the injection and extraction of minority carriers.
size 12{n=p=n rSub { size 8{i} } prop "exp" \( - { {E rSub { size 8{g} } } over {2k rSub { size 8{B} } T} } \) } {}
[4-1]
size 12{n&p&n rSub { size 8{i} } " are the electron, hole & intrinsic concentrations respectively" "." } {}
size 12{E rSub { size 8{g} } " is the gap energy, "T" is Temperature" "." } {}
size 12{ ital "pn"=n rSub { size 8{i} rSup { size 8{2} } } } {}
[4-2]